Name and formula

Reference code:	04-0477

Mineral name:	Anatase, syn

PDF index name:	Titanium Oxide

Empirical formula:	O2Ti

Chemical formula:	TiO2

Crystallographic parameters

Crystal system:	Tetragonal

Space group:	I41/amd

Space group number:	141

a (?):	  3.7830

b (?):	  3.7830

c (?):	  9.5100

Alpha (?):	 90.0000

Beta (?):	 90.0000

Gamma (?):	 90.0000

Calculated density:	  3.90

Volume of cell:	136.10

Z:	  4.00

RIR:	-

Status, subfiles and quality

Status:	Marked as deleted by ICDD

Subfiles:	Inorganic

Mineral

Alloy, metal or intermetalic

Quality:	Indexed (I)

Comments

Deleted by:	Continuation of 4-474.

Delete: Berry parcel February 5, 1959.

Optical data:	B=1.524, Q=1.5195, Sign=-

References

Primary reference:	Swanson, Tatge., Private Communication, (1950)

Additional pattern:	Parker., Z. Kristallogr., 59, 1, (1923)

Peak list

No.    h    k    l      d [A]       I [%]

1    1    0    1      3.51000     100.0

2    1    0    3      2.43500       9.0

3    0    0    4      2.37900      22.0

4    1    1    2      2.33600       9.0

5    2    0    0      1.89100      33.0

6    1    0    5      1.69900      21.0

7    2    1    1      1.66500      19.0

8    2    1    3      1.49400       4.0

9    2    0    4      1.48000      13.0

10    1    1    6      1.36700       5.0

11    2    2    0      1.33700       5.0

12    2    1    5      1.26400      10.0

13    3    0    1      1.25000       3.0

14    3    0    3      1.17100       2.0

15    3    1    2      1.16090       3.0

16                     1.08690       3.0

17    3    2    1      1.04330       3.0

18    1    0    9      1.01730       2.0

19    3    1    6      0.95500       4.0

20    4    0    0      0.94610       3.0

21    3    2    5      0.91890       2.0

22    1    1   10      0.89600       3.0

23    2    2    8      0.88770       2.0

24    3    2    7      0.83110       1.0

25    4    1    5      0.82680       3.0

26    3    0    9      0.81000       1.0

27                     0.79900       3.0

Stick Pattern